## Slide 1: Potential of 2D Dichalcogenides for Future Electronics
Goran Karapetrov
Department of Physics
Department of Materials Science and Engineering
Drexel University
Boston, MA Jan 13-15, 2025
Quantum Information Science on the Intersections of Nuclear and AMO Physics

## Slide 2
Motivation for using Ising Superconductors in NP
Ising Superconductivity in 2D Materials
Experimental Setup & Results
Outlook
Outline
Supported by DOE – NP DE-SC0023667

## Slide 3: Our Research Group - Current Research Areas
Engineered Correlated Electron Systems
Charge Density Wave Materials
Novel Superconducting Materials

## Slide 4: Growth of Single Crystal Dichalcogenides
TiSe2
TaS2
NbSe2
2I2(g) + Ti(s) + 2Se(s) → TiI4(g) + Se2(g) → TiSe2(s) + 2I2(g)
Thin film growth using chemical vapor transport

## Slide 5: UHV Scanning Probe Microscopy
5
UHV 10-11 Torr
minimum temp. 30K
E-beam evaporators
LEED/Auger, e-beam heating, etc

## Slide 6: Ultrafast Dynamics: Ultrafast Electron Diffraction
R. Ernstorfer, M. Harb, C. T. Hebeisen, G. Sciaini, T. Dartigalongue and R. J. D. Miller, Science (2009)
L. P. René de Cotret, et al., Advanced Structural and Chemical Imaging 4 (1), 11 (2018)

## Slide 7: Particle and Single Photon Detectors in High Magnetic Fields
Precision measurements require large magnetic fields. This demands field-resistance photon detectors for particle identification devices such as RICH detectors

## Slide 8: Superconductivity
Magnetic Field
Hc2
Hc1
Temperature
Tc
Normal State
Meissner State
Lower critical field
Vortex State
Upper critical field
DT
D R
SC transition

## Slide 9: Singlet Superconductors in High Magnetic Fields
Orbital effect (Lorentz force)
Paramagnetic effect (singlet pair)
B
-p
FL
p
FL
Sz=+1/2
Sz=-1/2
μBHc2~Δ~Tc
Kinetic energy of the supercurrent exceeds the superconducting gap energy
Spin paramagnetism exceeds the condensation energy of Cooper pair

## Slide 10: Superconductivity Beyond : Overcoming Pauli Limit
FFLO superconductivity (Fulde-Ferrel-Larkin-Ovchinnikov state)
Spin Triplet superconductivity
Spin-orbit scattering
Spin-orbit coupling (Ising superconductivity)
Sz=+1/2
Sz=-1/2

## Slide 11: FFLO Superconductivity
Non-zero momentum Cooper pairs giving rise to inhomogeneous superconductivity
H.A. Radovan et al. Nature 425 (2003) 51
Requirement: coherence length << mean free path (clean limit)

## Slide 12: Spin Triplet Superconductivity
Sz=+1/2
Sz=-1/2
Sz=+1/2
Sz=+1/2
Singlet Cooper pair (s=0)
Triplet Cooper pair (s=1)
URhGe
Aoki et al. Nature 413 (2001) 613

## Slide 13: Ising Superconductivity
Intrinsic spin-orbit coupling induced Zeeman field (locks the spins of Cooper pairs in opposite directions in opposite corners K, -K)
Effective Zeeman field prevents the alignment of the spins in the plane when in-plane magnetic field is applied (protects the superconducting state)
In-plane upper critical field overcomes Pauli limited:

## Slide 14: Necessary Ingredients for Ising Superconductivity
Upper critical field Bc2 enhancement is caused by spin-orbit coupling (SOC)
Spin-orbit coupling can be:
- Zeeman type
- Rashba type
Broken space inversion symmetry brings in effective crystalline field
(effective Zeeman field ):
Yuan et al. Nature Phys 9 (2013) 563

## Slide 15: Materials Hosting Ising Superconductivity
Monolayers (with large SOC and broken inversion symmetry)
Bulk quasi-2D crystals with alternating SOC/buffer layers
Bulk 2D crystals intercalated with molecules to decouple individual layers
Non-Ising: amorphous thin films (with large spin-orbit scattering i.e. spin randomization)

## Slide 16: Basic Properties of 2H-NbSe2
RRR ~ 100
Tc CDW = 33.5 K
Tc SC = 7.2 K
CDW
SC
17.2 nm x 17.2 nm T=4.2K
H.N.S. Lee et al., JAP 40 (1969) 602
p-type
n-type
M. Iavarone et al., JPCM 22 (2009) 015501
5%  R
Incommensurate CDW

## Slide 17: Electronic Structure of NbSe2 Monolayers
absence of inversion symmetry + spin-orbit coupling = band splitting
top view
side view
D. Wickramaratne et al. PRX 10 (2020) 041003

## Slide 18: Ising Superconductivity in Monolayers of Transition Metal Dichalcogenides (2H-NbSe2, 2H-MoS2…)
Xi et al. Nat Phys 12 (2016) 139

## Slide 19: Ising Superconductivity in Intrinsic Bulk Materials
P. Samuely et al. PRB 104 (2021) 224507

## Slide 20: Ising Superconductivity in Intrinsic Bulk Materials
R.T. Leriche al. Adv. Funct. Mater. 31 (2021) 2007706
LaSe buffer layers provide massive amount of e- to NbSe2 layers

## Slide 21: Ising Superconductivity in Artificially Structured Materials
Decoupling the lattice unit layers to achieve: (1) breaking of inversion symmetry
(2) doping
Decoupling of NbSe2 monolayers through MBE growth
Decoupling of NbSe2 monolayers through intercalation

## Slide 22: Ising Superconductivity in Fabricated Materials
Decoupling of NbSe2 monolayers through intercalation
Zhang et al. Nat Phys. 18 (2022) 1425
Yu et al. ACS Appl Mat Interf 16 (2024) 5904

## Slide 23: Ising Superconductivity in Artificially Structured Materials
Decoupling the lattice unit layers to achieve: (1) breaking of inversion symmetry
(2) doping
Decoupling of NbSe2 monolayers through MBE growth
Decoupling of NbSe2 monolayers through intercalation
Xing et al. Nano Lett. 17 (2017) 6802

## Slide 24: Electrochemical Intercalation of NbSe2 Single Crystal
NbSe2 intercalation with organic molecules
Current-Voltage graph of intercalating NbSe2 and diagram of intercalation process in the ionic liquid
Zhang et al. In: Nat Phys 18 (2022) 1425

## Slide 25: Electrochemical Intercalation of NbSe2 with [C2MIm]+
NbSe2 single crystal
Pt electrode
Nail polish
Optical image of the single crystal after 1 hour intercalation

## Slide 26: SNSPD Device Fabrication
Gold electrodes after lift-off​
NbSe2 flake transfer onto the substrate

## Slide 27: Single-Photon Measurement Probe
Probe coupled with PPMS

## Slide 28: Experimental setup for single-photon detection
Experimental setup:
Bias circuit
  Voltage supply w/ RLOAD)
  Bias-T
Optical setup
  Repetition modulator
  Laser
  Optical attenuator
Readout circuit
  LNA
  Oscilloscope/counter
SNSPD bias and readout circuit

## Slide 29: Preliminary Data
Next step – SNSPD patterning and single photon detection

## Slide 30: Future Outlook - Potential Ising Superconductors
Wang et al. Acc. Mater. Res. 2 (2021) 526

## Slide 31: Conclusions
Many opportunities (and challenges) in utilizing 2D materials in single photon/particle detection:
High magnetic field applications
Strong light-matter interactions (excitonic)
Intrinsically planar – stacked structures for sensing devices
Potential challenges:
Synthesis on planar substrates
Stability (temperature/radiation)?
Supported by DOE – NP DE-SC0023667

## Slide 33: Ising with FFLO